	Product Specification Sheet


	[image: image1.emf]




OWS- CaCO³ 101

Calcium Carbonate

PRODUCT DESCRIPTION:-

Finely ground white crystalline powder free from dirt and grits. Can be supplied in Fine Medium & Course Grades.
Calcium Carbonate is used as an acid soluble weighting agent in workover and completion fluids. Five different grades 45 ,100, 200, 300 and 400 mesh are supplied which differ only in their particle size distribution.

As weighting agent CaCo3 can be used to extend the brine’s maximum weights. As a bridging agent, the correct biend of 100, 200, 300 and 400 mesh grade can be used effectively seal the pores in the production formation, thus minimizing the invasion fluid. Because the material is derived from marble a metamorphic and highly crystalline form of calcium carbonate it does not break down in the high shear conditions encountered in drilling.

Breakdown of weaker materials derived from other sources, leads to increased invasion of the producing formation
	
PRODUCT SPECIFICATION
Property Description

Property Value/Quality

Specific Gravity                                      
2.71 kg/l 
Bulk density                                           
928-992 kg/m3

 (58-62 lbs/lt2)
CaCo3
95% min, 98% max
Water solublecontent                             
0.1%
PH at 10% solids                                   
10.0
* other details as well as MSDS available on request.
DISTRIBUTION
Oil & Water Supplies Limited

64 Angus Oval

Glasgow , G52 3HG

United Kingdom

Tele:+44 141 427 6416

Mob:+44 7789 958420

Fax: +44 141 427 7454

Email: sales@owsupplies.biz

	CERTIFICATION / APPROVAL

ISO 9001 : 2000 Approved
DOSING
As required
HANDLING / SAFETY
The handling of any chemical requires care. Anyone responsible for using or handling CaCO³ 101 should familiarize themselves with the full safety precautions outlined in our Material Safety Data Sheet. 

PACKAGING

Available in 25 kg,1,000 and 1,500 Kg Jumbo bags
STORAGE
Store in a dry, cool well ventilated area
.


See Website @ www.owsupplies.biz for full range of drilling agents
                                                  .

